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GEMINI 8018'G AWSISFAS5.5 E 8018-G

Typical Applications And Characteristics
GEMINI 8018-G is a basic coated hydrogen controlled clectrode for welding
low-alloy creepresisting CrMoV-steels. Maximum operation temperature 550° C.

Good weldability in all-position. Low spatter loss, ready slag detachment. Keep the
DC welding by preference.

Typical Al Weld Metal Properties

Composition Mechanical
()

0.06 Yield stress

140 Tensile strength
0.3 Elangation
050 CVN Impast Energy

Typical welding current

26x300 | 26x3%0
100 100

Calar End Purple

Cading side Gray

Printing G-3018-G/E BIEG

Welding Flat, harizantal, and vertical-up
Pasitians





