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HILCO AL Si5

TIG rods — aluminium

AWS A5.10: ER 4043
EN ISO 18273: S Al 4043A (AISi5(A))
Werkstoffnr. 3.2245

Wire type: Current: Welding positions:
TIG Solid wire h—-

~

Shielding gas:
11 =Pure Ar

AL Si 5 is aluminium wire for TIG welding, repairing and surfacing forged and cast aluminium-siicon alloys and
joining dissimilar aluminium alloys with max. 7%Si content. The easy flowing characteristics make the wire suitable
for welding all aluminium castings (except AMg castings). This type can be used in combination with tungsten
electrodes type WP,

Base materials to be welded: Applications:

« Auminium-Mgsi alloys « General fabrication & construction
o Alur m-Mg alloys up to 2,5% Mg (aluminium base metals)

« Aluminium-MnCu alloys « Shipbuilding & Offshore

« Aluminium-Si cast alloys « Repair & Maintenance

« Joining dissimilar aluminium alloys

Chemical composition, wt.% weld metal - typical:

Mechanical properties, weld metal — typical:
Condition 0,2% Yield strength | Tensile strength | Elongation Physical properties
MPa MPa Lo=5d - %
‘As welded =40 =120 =8 Melling range | _Density

573-625°C_| ~2680 kg/m®

Note: electrical conductivity 15-19 Sm/mm?

Packaging data:
i Weight / package
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