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Typical Applications And Characteristics

GEMINI 9018-G is  basic coated hydrogen controlled clectrods for fine grain
stecls having 2 tensile strength of 640-735 Nimm' .The deposited metal has an
excellent impact value. Steels that are sensitive to heat-input must be welded with
minimum of weaving. Low spatter loss with casy slag removal. DC welding by
preference.
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