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Costing type: current
Special
=+
A voltage: 65V
Tip colour:

HILCO Aluminil Si12

Stck electrodes - aluminium

AWS A5.3. E 4047
EN ISO 18273: E Al 4047 (AISi12)
DIN 1732: ELAISi 12
Werkstoffnr. 32585

ing positions:

e

Printing:

Alumini Si 12 is our special coated electrode developed for welding all types of aluminium castings and
applications where good colour matching with base maerial s important. Typical applications include repair
welding, surfacing and construction welding: window frames, aluminium tubes, fumiure, aluminium castings,
engine blocks, automoive parts. The electiode has a pure while coating specifcaly designed o reduce maistur
pick-up. For thicker plate materias (215 mm) it recommende to peheat at 150°C to 250°C before welding

Base materials to be welded: Applications
« Aluminium-Si cast alloys up 1o 12% Si content: .

G-AISI 12 (Cu), G-AISi 10 Mg (Cu), G-AISi 6 Cu 4 .

Equivalent product in alternative welding process:

‘General fabrication & consruction
Repair & Maintenance

SMAW GMAW FCAW GTAW SAW Cas wetding |
brazing
= ALSiT2 Z A2 5 ALS 12
Chemical composition, wt. % weld metal - typical:
C [ W [ s [ s [ P [ o [ W [ ™M [ cu [N [ VA
010 | 120 005 Bal
Note Zn 0.10 - Fe 040
Mechanical properties, weld metal - typical:
Condition | 0,2% Yield strength | _Tensit strength Elongation Wardnoss,
MPa MPa %
s welded 280 % 180 25 I
Packaging and welding data:
Dia. Length | Weight (kgs) | Current
mm. mm. 1000 pes. A
350 88 5090
350 152 50-110
350 196 110150
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