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Wire type:
OAW Solid wire

Shielding gas:
Oxy-acetylene

HILCO AL Si5 (OXY)

Gas welding rods ~ aluminium

AWS A5.10: ER 4043
EN ISO 18273: S Al 4043A (AISI5(A))
Werkstoffnr. 3.2245

-

AL Si 5 is aluminium wire for oxy-acetylene gas welding, repairing and surfacing forged and cast aluminium-silicon
alloys and joining dissimilar aluminium alloys with max. 7% Si content. The easy flowing characteristics make the
wire suitable for welding all aluminium castings (except AIMg castings).

Base materials to be welded:

Chemical compos

Aluminium-MgSi alloys
Aluminium-Mg alloys up to 2,5% Mg
Aluminium-MnCu alloys
Aluminium-Si cast alloys

Joining dissimilar aluminium alloys

n, wt.% weld metal - typical:

Applications:
General fabrication & construction
(aluminium base metals)
Shipbuilding & Offshore
Repair & Maintenance

Mn Si Fe Cu Al
0.15 50 060 030 Bal
Mechanical properties, weld metal — typical:
Condition 0,2% Yield strength | Tensile strength | Elongation Physical properties
MPa MPa Lo=5d - %
"As welded =70 >130 >16 | Meling range | _Density
573-625°C_| ~2680 kg/m®

Packaging data:
Dia. Length Weight ] package
mm. mm. kg.

16 1000 5 |
20 1000 5 |
24 1000 5 |
L 32 1000 5 |
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