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HILCO AL 99,7

TIG rods — aluminium

EN SO 18273: S Al 1070 (A 99,7)
Werkstoffnr. 3.0275

Wire type: Current: Welding positions:
TIG Solid wire —
~ {
Shielding gas:
11 = Pure Ar

AL 99,7 is our aluminium wire for TIG welding pure aluminium and wrought aluminium alloys. Highly resistant
to chemical attack and weathering. It is a relatively soft alloy that is very formable and it is used extensively in
thin-gauge and foil products. Deposit weld metal has good mechanical properties. Typical applications include
repair welding engine blocks, oil-castings, automotive parts and aluminium pump housings. To be used in
combination with tungsten electrodes type WP,

Base materials to be welded: Applications:

« Pure aluminium Al 99,5, Al 99,7, Al 99,8 and Al 99 « General fabrication & construction
«  Pure aluminium Werkstoffnr. 3.0255, 3.0275, 3.0285 and 3.0205 «  (aluminium base metals)

«  Similar aluminium and wrought aluminium alloys «  Repair & Maintenance

Condition 0,2% Yield strength | Tensile strength | Elongation Physical properties
MPa MPa Lo=5d - %

As welded 235 =75 =45 Melting range | Density
647-558°C | ~2700 kg/m®

Note: electrical conductivity 33 Sm/mm?*

Packaging data:
Dia. Length Weight / package
mm. mm. kg.
1.6 1000 5
2,0 1000 5
24 1000 5
32 1000 5
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